Supplementary Material

Table 1. Catalytic Systems Used in First Screening Experiments.

| Exp # | Metal | Supplier | Code | T (°C) | Average Da |
| --- | --- | --- | --- | --- | --- |
| a1 | Ru/C | Sigma | 84031 | 140 | 4.7 |
| a2 | Ru/C | Johnson Matthey | 5R600 | 140 | 4.3 |
| a3 | Ru/C | Johnson Matthey | 5R619 | 140 | 4.8 |
| a4 | Ru/C | Evonik | P3059 | 140 | 4.0 |
| a5 | Ru/C | Evonik | P3060 | 140 | 4.2 |
| a6 | Ru/C | BASF | 4401 | 140 | 4.3 |
| a7 | Ru,Pd/C | Johnson Matthey | 5R611 | 140 | 4.0 |
| a8 | Pd/C | Evonik | P1070 | 140 | 1.4 |
| b1 | Pd/C | Johnson Matthey | 10R39 | 140 | 0.9 |
| b2 | Pd/C | Evonik | P1092 | 140 | 0.6 |
| b3 | Pd/C | Hindustan Platinum | RD-169 | 140 | 0.6 |
| b4 | Pd/C | BASF | 1951 | 140 | 0.4 |
| b5 | Rh/C | Sigma | 206164 | 140 | 3.5 |
| b6 | Rh/C | Hindustan Platinum | RD-199 | 140 | 1.3 |
| b7 | Rh/C | Johnson Matthey | 5R20A | 140 | 1.2 |
| b8 | Rh/C | Evonik | P3053 | 140 | 2.3 |
| c1 | Ru/C | Sigma | 84031 | 180 | 5.8 |
| c2 | Ru/C | Johnson Matthey | 5R619 | 180 | 4.8 |
| c3 | Pd/C | Evonik | P1070 | 180 | 4.0 |
| c4 | Pd/C | Johnson Matthey | 10R39 | 180 | 3.3 |
| c5 | Rh/C | Sigma | 206164 | 180 | 5.9 |
| c6 | Rh/C | Evonik | P3053 | 180 | 3.0 |
| c7 | Carbon | - | - | 180 | 0 |
| c8 | No catalyst | - | - | 180 | 0 |
| d1 | Rh/Al2O3 | HP | RD-8 | 180 | 2.4 |
| d2 | Pd/SiO2/Al2O3 | Johnson Matthey | 2R31 | 180 | 0.5 |
| d3 | Rh/Al2O3 | Johnson Matthey | 5R524 | 180 | 3.7 |
| d4 | Ru/Al2O3 | Johnson Matthey | 5R698 | 180 | 4.2 |
| d5 | Pd/Al2O3 | Evonik | PMPC130524 | 180 | 1.6 |
| d6 | Pd/SiO2 | SiliCycle | R815-110 | 180 | 0.8 |
| d7 | PtO2 | Aldrich | 206032 | 180 | 2.4 |
| d8 | Ni | Grace | 2800 | 180 | 6.7 |
| e1 | Ni | Grace | 2800 | 160 | 5.5 |
| e2 | Co with Cr | Grace | 2724 | 160 | 1.9 |
| e3 | Ni with Mo | Grace | 3111 | 160 | 5.9 |
| e4 | Co with Ni | Evonik | MC201 | 160 | 2.4 |
| e5 | Ni with Fe, Cr | Evonik | MC502 | 160 | 6.5 |
| e6 | Ni | Johnson Matthey | HTC Ni 500 RP 1.2mm | 160 | 2.8 |
| e7 | Co | Johnson Matthey | HTC Co 2000 RP 1.2mm | 160 | 1.3 |
| e8 | Ni | Applied Catalysts | NB40-35-01 | 160 | 1.5 |
| f1 | Ni with Cr | Grace | 2400 | 160 | 6.9 |
| f2 | Ni | Grace | 5601 | 160 | 5.8 |
| f3 | Ni with Fe, Cr | Johnson Matthey | A-4000 | 160 | 5.2 |
| f4 | Ni | Johnson Matthey | A-5000 | 160 | 6.3 |

a This pertains only to the eight protons attached to the carbon atoms in morpholine.

Table 2. DOE Studies.

| Exp # | Loading (wt/wt)a | T (°C) | P (bar) | Time (h) | Average Db | GC %Purity |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 50 | 160 | 10 | 16 | 6.7 | 93.1 |
| 2 | 27.5 | 140 | 6 | 10 | 2.9 | 98.5 |
| 3 | 5 | 120 | 10 | 4 | 0.2 | 97.0 |
| 4 | 27.5 | 140 | 6 | 16 | 4.0 | 95.4 |
| 5 | 5 | 120 | 2 | 16 | 0.4 | 99.2 |
| 6 | 50 | 120 | 2 | 16 | 2.7 | 98.4 |
| 7 | 27.5 | 140 | 6 | 4 | 1.5 | 97.8 |
| 8 | 27.5 | 140 | 2 | 10 | 3.6 | 95.6 |
| 9 | 5 | 160 | 10 | 4 | 0.9 | 98.4 |
| 10 | 50 | 160 | 2 | 4 | 7.0 | 95.5 |
| 11 | 5 | 160 | 10 | 16 | 1.7 | 96.8 |
| 12 | 50 | 120 | 2 | 4 | 1.7 | 98.7 |
| 13 | 27.5 | 120 | 6 | 10 | 0.6 | 97.7 |
| 14 | 5 | 120 | 10 | 16 | 0.3 | 97.4 |
| 15 | 50 | 140 | 6 | 10 | 4.5 | 96.2 |
| 16 | 5 | 140 | 6 | 10 | 0.6 | 96.9 |
| 17 | 5 | 160 | 2 | 16 | 2.4 | 97.5 |
| 18 | 5 | 120 | 2 | 4 | 0.2 | 96.4 |
| 19 | 27.5 | 140 | 10 | 10 | 1.1 | 98.4 |
| 20 | 27.5 | 160 | 6 | 10 | 6.5 | 94.7 |
| 21 | 50 | 160 | 2 | 16 | 7.5 | 89.1 |
| 22 | 50 | 120 | 10 | 4 | 0.4 | 98.6 |
| 23 | 50 | 120 | 10 | 16 | 1.1 | 99.8 |
| 24 | 50 | 160 | 10 | 4 | 4.9 | 97.7 |
| 25 | 27.5 | 140 | 6 | 10 | 2.7 | 96.6 |
| 26 | 5 | 160 | 2 | 4 | 1.6 | 99.1 |

a Weight of catalyst as a percentage of the weight of morpholine, which is approximately 0.2 g.

b This pertains only to the eight protons attached to the carbon atoms in morpholine.

Characterization of Final Morpholine-d8

Purity determination by chromatography. GC purity was determined using an Agilent DB-1, column (0.25 mm ID x 30 m, 1 µm film). A mixed basic solution was used to ensure neutralization and volatilization of the hydrochloride salt (0.5 M aqueous NaOH/MeOH 1:4).

Determination of deuterium incorporation. The deuterium content was determined using two orthogonal methods: while the NMR method indicated a deuterium incorporation of 97.6%, the LC-MS method resulted in 95.6%. Based on these results, we estimated the total deuterium incorporation to be 96%.

LC-MS method. Purified samples were derivatized with dansyl chloride and analyzed by LC-MS using a generic UPLC method (0.1% formic acid in water and acetonitrile (ACN) on a Waters Acquity UPLC BEH column, C18, 2.1 x 50 mm, 1.7 µm at 220 nm). The relative molar amounts of partially and fully deuterated species (d5, d6, d7, d8) were determined by analysis of the isotopic distribution pattern ([M + H]+); a weighted sum was used to calculate the degree of deuteration (see below).

= SD Weighting (N) X Relative Abundance (N), where N = 1 to 8

= D Weighting (D6) X Relative Abundance (D6) + D Weighting (D7) X Relative Abundance (D7)

+ D Weighting (D8) X Relative Abundance (D8)

NOTE: At high Deuteration, D1 – D5 terms become insignificant and are omitted

whereby

%D 			= % Deuterium Incorporation in Morpholine Ring

D Weighting		= Deuterium Weighting

= Deuterium incorporation vs theoretical

= N/8

= E.g. For D7, D Weighting = 7/8 = 0.875

Relative Abundance		= Signal response of deuterated compound relative to total signal response

1H/2H-NMR spectroscopy. Samples were analyzed in D2O on a Bruker AVANCE III-HD 400 MHz/54 mm spectrometer using an extrinsic internal standard (composite of CH3CN and CD3CN of a known and controlled ratio, signal at 1.97 ppm in D2O). An extended d1 was used (60 s) to avoid signal saturation. The area ratio of the morpholine signals relative to the acetonitrile methyl peaks was measured in both the 1H and 2D spectra. The total deuterium incorporation was calculated by comparison of these ratios, i.e. the degree of deuterium incorporation at each morpholine ring position (OCH2 vs. NCH2: signals at 3.21 and 3.86 ppm, respectively).

2H1HPositionMorpholine - d8=(Morpholine-d8 2HPeak(ACN  2H Peak) 2H1HRatio of ACN standardMorpholine-d8 2H Peak(ACN 2H Peak) 2H1HRatio of ACN standard+ (Morpholine-d8  1H Peak) (ACN 1H Peak) )

2H1HTotalMorpholine - d8=#H at position#H in Morpholine-d82H1HPositionMorpholine- d8+#H at position#H in Morpholine-d82H1HPositionMorpholine - d8

2H1HTotalMorpholine - d8=#H at OCH282H1HOCH2Morpholine - d8+#H at NCH282H1HNCH2Morpholine - d8

2H1HTotalMorpholine - d8=482H1HOCH2Morpholine - d8+482H1HNCH2Morpholine - d8

whereby

Morpholine-d8 2HPeak  	= integration value of morpholine peak in 2H spectrum

Morpholine-d8  1H Peak 	= integration value of morpholine peak in 1H spectrum

ACN  2H Peak  		= integration value of ACN peak in 2H spectrum

ACN  1H Peak  		= integration value of ACN peak in 1H spectrum

2H1HRatio of ACN standard  	= ratio of  1H and 2H in ACN standard based on isotopic purity of CD3CN and ratio of CD3CN and CH3CN used to prepare standard

13C-NMR spectroscopy of morpholine-d8 hydrochloride (100.6 MHz, D2O): δ 42.5 (N−CD2, JC,D = 22.1 Hz), 62.7 (N−CD2, JC,D = 22.1 Hz); comparison with non-deuterated morpholine hydrochloride (D2O): δ 43.2 (N−CD2), 63.1 (N−CD2).